## Slide 1
油井水泥降失水剂
发布日期： 2024-6-10
C-FL90S是C-FL90L的固体粉末，可控制低温至高温水泥浆体系的失水量，特别适合在盐水中使用。
本信息仅供参考，COSL对该部分的信息不做任何担保和保证。
所有涉及到的产品和质量保障应遵守销售条款。本文件中的内容不具法律效应，也不是有效的法律建议。
理化性能 | 
外观 | 黑色粉末
密度, g/cm3 | 1.35±0.05
pH值（1%水溶液) | 6.0-7.0
技术说明书
主要特性
可使用淡水和饱和盐水配浆
具有辅助分散的性能
包装储运
包装要求：复合包装袋或按用户要求
包装规格：25kg/袋或按用户要求
贮存条件：贮存在干燥通风处，远离热源、火源
保 质 期：12个月
应用范围
推荐温度（BHCT）：20-230℃（68-446℉）
推荐加量（BWOC）：0.7-3.5%
C-FL90S
www.cosl.com.cn
中海油田服务股份有限公司
河北省廊坊市三河燕郊行宫西大街81号
zhangxd11@cosl.com.cn
+86-10-8452 2344

## Slide 2
OIL WELL CEMENT FLUID LOSS ADDITIVE
Date issued： 2024-6-10
C-FL90S
C-FL90S is the solid form of C-FL90L, which is used to control the fluid loss of cement slurries from low temperature to high temperature, especially suitable used in salt water.
FEATURES
Suitable for mixing with fresh water and saturated salt water
Asists to disperse ccement slurry
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
APPLICATION
Recommended temperature (BHCT): 68 -446℉ (20-230℃)
Recommended dosage (BWOC): 0.7-3.5%
PACKAGE & STORAGE
Specifications of packaging: Composite packaging bag or as per client's requirements
Packing size: 25 kg/sx (55 lb/sx) or as per client's requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
Period of validity: 12 months
Specification | 
Appearance | Black powder
Density, g/cm3 | 1.35±0.05
pH (1% aqueous solution) | 6.0-7.0