## Slide 1
油井水泥降失水剂
发布日期： 2024-6-10
C-FL87L是一种分散型聚合物类降失水剂，可用于控制水泥浆的失水量。
本信息仅供参考，COSL对该部分的信息不做任何担保和保证。
所有涉及到的产品和质量保障应遵守销售条款。本文件中的内容不具法律效应，也不是有效的法律建议。
理化性能 | 
外观 | 无色或淡黄色液体
密度, g/cm3 | 1.10±0.02
pH值 | 6.0-7.0
技术说明书
主要特性
有效控制失水量和游离液
淡水或盐水配浆均可
具有辅助分散的性能
包装储运
包装要求：塑料桶或按用户要求
包装规格：1000L/桶或按用户要求
贮存条件：贮存在干燥通风处，远离热源、火源
保 质 期：24个月
应用范围
推荐温度（BHCT）：30-130℃（86-266℉）
推荐加量（BWOC）：3.0-8.0%
C-FL87L
www.cosl.com.cn
中海油田服务股份有限公司河北省廊坊市三河燕郊行宫西大街81号
zhangxd11@cosl.com.cn
+86-10-8452 2344

## Slide 2
OIL WELL CEMENT FLUID LOSS ADDITIVE
Date issued： 2024-6-10
C-FL87L is a kind of polymer fluid loss additive used to contol the fluid loss of slurry.
FEATURES
Effectively controls fluid loss and free water
Suitable for mixing with fresh water and salt water
Asists to disperse cement slurry
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
APPLICATION
Recommended temperature (BHCT): 86-266℉ (30-130℃)
Recommended dosage (BWOC/gps): 3.0-8.0%/0.307-0.819
PACKAGE & STORAGE
Specifications of packaging: Plastic drum or as per client's requirements
Packing size: 1000 L/drum or as per client's requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
Period of validity: 24 months
Specification | 
Appearance | Colorless or yellowish liquid
Density, g/cm3 | 1.10±0.02
pH | 6.0-7.0
C-FL87L