## Slide 1
油井水泥降失水剂
C-FL80S是C-FL80L的固体粉末，是一种聚合物类降失水剂，可用于控制水泥浆的失水量。
主要特性
可有效控制失水量和游离液
淡水或盐水配浆均可
有助于提高水泥浆稳定性和流变性
本信息仅供参考，COSL对该部分的信息不做任何担保和保证。
所有涉及到的产品和质量保障应遵守销售条款。本文件中的内容不具法律效应，也不是有效的法律建议。
发布日期： 2024-6-10
理化性能 | 
外观 | 白色或淡黄色粉末
密度, g/cm3 | 1.25±0.05
pH值 | 6.0-7.0
水溶性 | 可溶
技术说明书
包装储运
包装要求：复合包装袋或按用户要求
包装规格：25kg/袋或按用户要求
贮存条件：贮存在干燥通风处，远离热源、火源
保 质 期：24个月
应用范围
推荐温度（BHCT）：30-230℃（86-446℉）
推荐加量（BWOC）：0.6-2.5%
C-FL80S
www.cosl.com.cn
中海油田服务股份有限公司
河北省廊坊市三河燕郊行宫西大街81号
zhangxd11@cosl.com.cn
+86-10-8452 2344

## Slide 2
OIL WELL CEMENT FLUID LOSS ADDITIVE
C-FL80S is the solid form of C-FL80L, which is a kind of polymer fluid loss additive used to control the fluid loss of slurry.
FEATURES
Effectively control fluid loss and free water
Suitable for mixing with fresh water and salt water
Asists to improve slurries stability and rheology
Date issued： 2024-6-10
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
APPLICATION
Recommended temperature (BHCT): 86-446℉ (30-230℃)
Recommended dosage (BWOC): 0.6-2.5%
PACKAGE & STORAGE
Specifications of packaging: Composite packaging bag or as per client's requirements
Packing size: 25 kg/sx (55 lb/sx) or as per client's requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
Period of validity: 24 months
C-FL80S
Specification | 
Appearance | White or yellowish power
Density, g/cm3 | 1.25±0.05
pH (1% aqueous solution) | 6.0-7.0
Solubility in water | Soluble