## Slide 1
C-F46S
油井水泥分散剂
发布日期： 2024-6-10
C-F46S是C-F46L的固体粉末，可用于降低水泥浆黏度，改善不同温度段水泥浆的流变性能。
本信息仅供参考，COSL对该部分的信息不做任何担保和保证。
所有涉及到的产品和质量保障应遵守销售条款。本文件中的内容不具法律效应，也不是有效的法律建议。
理化性能 | 
外观 | 红棕色固体
密度，g/cm3 | 1.20±0.02
pH值 (1%水溶液) | 12.0-14.0
技术说明书
主要特性
有效改善流变性能
对稠化时间及抗压强度影响小
适用于淡水或盐水配浆
与大多数COSL固井外加剂相容性良好
包装储运
包装要求：复合包装袋或按用户要求
包装规格：25kg/袋或按用户要求
贮存条件：贮存在干燥通风处，远离热源、火源
保 质 期：24个月
应用范围
推荐温度（BHCT）：≤230℃（≤446℉）
推荐加量（BWOC）：0.2-1.0%
避免与C-FL71L/C-FL72L降失水剂一起使用
www.cosl.com.cn
中海油田服务股份有限公司
河北省廊坊市三河燕郊行宫西大街81号
zhangxd11@cosl.com.cn
+86-10-8452 2344

## Slide 2
OIL WELL CEMENT DISPERSANT
Date issued： 2024-6-10
C-F46S
C-F46S is solid form of C-F46L, which reduces the apparent viscosity and improve the rheological property of the cement slurries.
FEATURES
Effectively reduces the slurry viscosity and improve the rheological properties
Low influence on thickening time and compressive strength
Suitable for mixing with fresh water and salt water
Good compatibility with most COSL cementing additives
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
APPLICATION
Recommended temperature (BHCT): ≤446℉ (≤230℃)
Recommended dosage (BWOC): 0.2-1.0%
Avoid of using together with C-FL71L
PACKAGE & STORAGE
Specifications of packaging: Composite packaging bag or as per client's requirements
Packing size: 25 kg/sx (55 lb/sx) or as per client's requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
Period of validity: 24 months
Specification | 
Appearance | Reddish brown solid
Density, g/cm3 | 1.20±0.02
pH (1% aqueous solution) | 12.0-14.0