## Slide 1
C-GS12L
油井水泥防气窜剂
发布日期： 2024-6-10
C-GS12L 是一种硅质类防气窜剂，可有效防止发生气窜，并提高水泥石抗压强度。
www.cosl.com.cn
中海油田服务股份有限公司
河北省廊坊市三河燕郊行宫西大街81号
zhangxd11@cosl.com.cn
+86-10-8452 2344
本信息仅供参考，COSL对该部分的信息不做任何担保和保证。
所有涉及到的产品和质量保障应遵守销售条款。本文件中的内容不具法律效应，也不是有效的法律建议。
理化性能 | 
外观 | 灰黑色液体
密度, g/cm3 | 1.38±0.02
pH值 | 6.0-7.0
技术说明书
主要特性
有效缩短水泥浆静胶凝发展过渡时间
提高水泥石抗压强度
提高水泥浆稳定性
包装储运
包装要求：塑料桶或按用户要求
包装规格：1000L/桶或按用户要求
贮存条件：贮存在干燥通风处，远离热源、火源
保 质 期：6个月
应用范围
推荐温度（BHCT）：≤230℃（≤446℉）
推荐加量（BWOC）：4.0-30.0%

## Slide 2
C-GS12L
OIL WELL CEMENT
ANTI-GAS MIGRATION ADDITIVE
Date issued： 2024-6-10
C-GS12L is a siliceous anti-gas migration additive, which mainly prevents gas migration and improves the mechanical properties of set cement.
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
FEATURES
Effectively shortens cement slurries transition time
Improves the compressive strength of cement stone
Improves the stability of cement slurries
PACKAGE & STORAGE
Specifications of packaging: Plastic drum or as per client’s requirements
Packing size: 1000 L/drum or as per client’s requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
Period of validity: 6 months
APPLICATION
Recommended temperature (BHCT): ≤446℉ (≤230℃)
Recommended dosage (BWOC/gps): 4.0-30.0%/0.324-2.431
Specification | 
Appearance | Grey or black liquid
Density, g/cm3 | 1.38±0.02
pH | 6.0-7.0