## Slide 1
PF-NSEAL
NANO-LATEX PLUGGING AGENT
Date issued: 2024-6-10
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
PACKAGE & STORAGE
Specifications of packaging: Plastic barrel as per client’s requirements
Packing size: 200 L per drum or as per client’s requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
PF-NSEAL is a nano type deformable polymer latex. It can be used in water-based and non-aqueous drilling fluid for sealing the nano pores and micro fractures of shales, thereby effectively reducing the pore pressure penetration and improve the shale stabilitty .
FEATURES
Reduce the invasion of water into the shale and impeove the shale stabilitty
Good thermal stability
Tolerant of high salinity
APPLICATION
Suitable for water-based and non-aqueous drilling fluids
Applicable temperature: ≤ 350 ℉
Recommended dosage: 3.5-10. 5ppb
Application limitation: not used for reservoir drilling fluid
Specification | 
Appearance | Milky white liquid
pH | 8-10
Specific gravity, g/cm3 | 1.02-1.04
Average particle size, nm | 200-500