## Slide 1
PE-LW21L
流态稳定剂
PE-LW21L可用于延长各种返排水泥浆的凝固时间，使返排的水泥浆长时间稳定在流动状态，便于返排水泥浆的海上转运，确保后期处理。
产品描述
性能特点
能有效延长水泥浆的凝固时间
能够确保返排的水泥浆长时间保持稳定的流动态
适用于各类密度水泥浆体系
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao, Sanhe, Hebei, China
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale. Nothing in this document is legal advice or is a substitute for competent legal advice.
应用范围
推荐加量:10 kg～40 kg/m3
与返排水泥浆混合均匀后，静置存放即可
包装储运
理化性能
项 目 | 指 标
外观 | 无色至浅黄色液体
密度（25±2℃），g/cm3 | 1.22～1.28
缓凝时间（24℃，常压），d | ≥15（未达终凝）
缓凝时间（40℃，常压），d | ≥15（未达终凝）
包装要求：塑料桶或按用户要求
包装规格：25 L/桶或按用户要求
贮存条件：贮存在干燥通风处，远离热源、火源
保 质 期：24个月
Notes: 1