## Slide 1
PF-GREENSEAL
LOST CIRCULATION MATERIAL(LCM) ENVIRONMENTAL-FRIENDLY
Date issued: 2024-6-10
PF-GREENSEAL is an environmental-friendly mixture of nano deformable particles and rigid particles. It can reduce pore pressure penetration and improve wellbore stability by sealing pores and micro fractures.
Technical Data Sheet
www.cosl.com.cn
China Oilfield Services Limited
No.81, Xinggong West Street, Yanjiao,
Sanhe, Hebei, China
zhangxd11@cosl.com.cn
+86-10-8452 2344
This information is supplied solely for informational purposes and COSL makes no guarantees or warranties, either expressed or implied, with respect to the accuracy and use of this data. All product warranties and guarantees shall be governed by the Standard Terms of Sale.
Nothing in this document is legal advice or is a substitute for competent legal advice.
PACKAGE & STORAGE
Specifications of packaging: Composite packaging bag or as per client’s requirements
Packing size: 25kg per sack or as per client’s requirements
Storage conditions: Store in dry area. Avoid open flame, strong oxidant, high-temperature environment
FEATURES
Effective sealing of microfractures
Reduce the pore pressure penetration
Improve wellbore stability
Environmental friendly
APPLICATION
Suitable for fresh water, salt water based drilling fluids
Applicable temperature: ≤ 300 ℉
Recommended dosage: 7-10.5 ppb
Restrictions: Not suitable for reservoir drilling fluids
Specification | 
Appearance | White free-flowing powder
Moisture，% | ≤5
Screen floating (325 mesh standard sieve)，% | ≤10
Acid solubility，% | ＞70